Sawngoods.

**Segezha Group** is а holding company, which comprises three sawmills located in North-West part of Russia, namely:

JSC “Sokol Timber Company” (STC), Vologda region of Russia, Sokol,

LLC “LDK Segezhsky”, Republic of Karelia of Russia, Segezha,

JSC “Onega sawmills”, Arkhangelsk region of Russia, Onega.

1. **Production of JSC “Sokol Timber Company”, Vologda region, Russia.**

Species:

Whitewood – ab.80%

Redwood – ab. 20%

Moisture content:

Kiln Dried 18% (+/-2%)

Quality (grading):

grade SF (ABC)

grade D/III 8486-86

grade IV 8486-86

Lengths:

2,70 – 6,00 m with a step of 30cm.

(sawngoods are produced from 6,00m (ab.90%) and 4,00m (ab.10%) logs, so that the main lengths of sawngoods (ab. 70%) are the lengths 5,10 – 6,00m).

Main cross-sections:

|  |  |  |
| --- | --- | --- |
| Thickness(mm) x width(mm) | Whitewood | Redwood |
| 63x150 | x |  |
| 50x200 |  | x |
| 50x150 | x | x |
| 50х125 |  | х |
| 50x100 |  | x |
| 47x150 | x |  |
| 47x125 | x |  |
| 47x100 | x |  |
| 44x150 | x |  |
| 44x125 | x |  |
| 44x100 | x |  |
| 38x150 | x |  |
| 38x100 | x |  |
| 32x150 | x | x |
| 32x100 | x |  |
| 25x150 | x | x |
| 25x125 | x | x |
| 25x100 | x | x |
| 19x100 | x |  |
| 15x100 | x | x |
| 15x75 | x | x |

Packing:

Packages – one length package (LP), 5-sides plastic wrapped. Maximum package size – 1150mm x 1150mm. Half- and quarter- packages are allowed.

Shipments of the goods can be made by trucks form the mill (DAP basis) and containers from St.Petersburg.

1. **Production of “Segezha sawmills” LLC, Karelia Republic, Russia.**

Species:

Whitewood – ab.40%

Redwood – ab. 60%

Moisture content:

Kiln Dried, max. 22%

Quality (Scandinavian grading rules):

* *for Redwood*

grades A, B, C, D

grade SF (ABC), D

grade VI (Domestic)

* *for Whitewood*

grade SF (ABC), D

grade VI (Domestic)

Lengths:

2,70 – 6,00 m with a step of 30cm.

(sawngoods are produced from 5,50m logs, so that the main lengths of sawngoods (ab. 70-75%) are the lengths 4,50/4,80/5,10/5,40m).

Main cross-sections:

|  |  |  |
| --- | --- | --- |
| Thickness(mm) x width(mm) | Whitewood | Redwood |
| 50x200 |  | x |
| 50x175 |  | x |
| 50x150 |  | x |
| 50x125 |  | x |
| 50x100 |  | x |
| 47x150 | x |  |
| 47x125 | x |  |
| 47x100 | x |  |
| 44x150 | x |  |
| 44x125 | x |  |
| 44x100 | x |  |
| 38x150 | x | x |
| 38x125 | x | x |
| 38x100 |  | x |
| 32x150 | x | x |
| 32x125 | x | x |
| 32x100 | x | x |
| 25x225 |  | x |
| 25x200 |  | x |
| 25x175 |  | x |
| 25x150 |  | x |
| 25x125 |  | x |
| 25x100 |  | x |
| 22x200 | x |  |
| 22x175 | x |  |
| 22x150 | x |  |
| 22x125 | x |  |
| 22x100 | x |  |

Packing:

Minimum 85% of the volume shall be 1 length per package (LP).

Packages of not more than 3 adjoining lengths should be packed “ladder like” (TP).

Packages having up to 5 boards 0,3 m. shorter than the rest of the boards in the package to be considered as length-packaged (Segezha standard).

For A, B, C, SF (ABC) grades - 5-sides plastic wrapped, for D, VI-VIII grades - top layer covered. Maximum package size – 1100mm x 1100mm. Half- packages are allowed.

Shipments of the goods can be made by vessels and trucks form the mill and by containers from St.Petersburg.

1. **Production of JSC “Onega sawmills” Archangel region, Russia.**

Species:

Whitewood – abt. 80%

Redwood – abt. 20%

Moisture content:

Kiln Dried, max. 22%

Quality (Scandinavian grading rules):

* *for Redwood*

grade SF (ABC), D

grade Domestic

* *for Whitewood*

grade SF (AB/ ABC), C, D

grade Domestic

Lengths:

2,70 – 6,00 m with a step of 30cm.

(main lengths of logs are 5,5/ 6,1 m).

Main cross-sections:

|  |  |  |
| --- | --- | --- |
| Thickness(mm) x width(mm) | Whitewood | Redwood |
| 75 x 225 | X | X |
| 75 x 200 | X | X |
| 63 x 175 | X |  |
| 63 x 150 | X | X |
| 50 x 150 | X | X |
| 50 x 125 | X | X |
| 50 x 100 | X | X |
| 47 x 150 | X |  |
| 47 x 125 | X |  |
| 47 x 100 | X |  |
| 44 x 225 | X |  |
| 44 x 175 | X |  |
| 44 x 150 | X |  |
| 44 x 125 | X |  |
| 44 x 100 | X |  |
| 38 x 200 | X |  |
| 38 x 150 | X | X |
| 38 x 125 | X | X |
| 38 x 100 | X | X |
| 36 x 147 | X |  |
| 36 x 122 | X |  |
| 36 x 112 | X |  |
| 36 x 97 | X |  |
| 35 x 150 | X |  |
| 35 x 100 | X |  |
| 32 x 150 | X | X |
| 32 x 100 | X |  |
| 25 x 225 |  | X |
| 25 x 200 |  | X |
| 25 x 175 |  | X |
| 25 x 150 |  | X |
| 25 x 125 |  | X |
| 25 x 100 |  | X |
| 25 x 75 |  | X |
| 22 x 200 | X |  |
| 22 x 175 | X |  |
| 22 x 150 | X |  |
| 22 x 125 | X |  |
| 22 x 100 | X |  |
| 19 x 100 | X | X |
| 19 x 75 | X |  |

Packing:

Minimum 85% of the volume shall be 1 length per package (LP).

Packages of not more than 3 adjoining lengths should be packed “ladder like” (TP).

For SF (AB / ABC), D grades - 5-sides plastic wrapped.

Package size – 1100mm x 1100mm.

Half- packages are allowed.

Shipments of the goods can be made by vessels form the mill and containers from St.Petersburg.